DC PN 008 – 4/1/2011 – ASPHALT BINDER CONTENT FOR PLANT MIX PAVEMENTS

On this project, design all asphalt concrete pavements requiring 441 in accordance with the provisions of 441.02, except that the following limits shall apply to asphalt binder content:

Asphalt Material Type	Asphalt Binder Content (Percent of Total Mix)

Type 1 Surface and Intermediate 	6.4 to 6.8

Type 2 Intermediate	5.5 to 5.9

The contractor's job mix formula (JMF) shall be submitted to the Engineer no less than 14 days prior to beginning work.